## Slide 1
H2-HBI
BOF
EAF
COOLSTAR* Project (Dec. 2017 ~ Feb. 2025)
Ministry of Trade, Industry and Energy
- Companies : POSCO, HYUNDAI Steel,..
- Universities, Research Institutes
※ COOLSTAR: CO2 Low emission technology of Steelmaking And hydrogen Reduction
○ Target : Develop technologies to reduce CO2 emissions(direct/indirect) by 15% in steelworks
○ Project Overview
Sub 1
Hybrid ironmaking technology based on BF
- H2 enriched gas injection
- Application of low reduced iron
Sub 2
H2 amplification based on by-product gas
Sub 3
BOF/EAF improvement based on substitution raw material
By-product gas
(H2 bearing gas)
Hot compacting
Fluidized bed
reduction
• Low-Reduced Iron
• Reducibility : 65~70 %
• Direct Reduction ↓
LRI production
Coke Oven
COG
(H2 56%, CH4 26%)
H2 containing gas
tuyere injection
LRI
Coke
Coke re-design
for H2 reduction
• Replacing C by H2
• BF H2 reduction↑
C rate ↓
Sinter
H2
Government-led
Project

## Slide 2
Technology Structure
Byproduct Gas
(Hydrogenous Gas)
Conversion to
reducing gas
Fluidized
bed
• Low-Reduced Iron(LRI)
• Reduction degree : 6570 %
• Decrease direct reduction
LRI manufacturing/charging technology
Coke Oven
COG
(H2 56%, CH4 27%)
• COG, FOG
Injection technology of hydrogenous gas
• Replacement of C by H2
• Increase indirect reduction
LRI
Coke
Biomass injection technology
• Use biomass, C neutral
as H2 source
Molten
iron
Biomass
CO2 utilization
Exhaust gas(CO2)
• Synthesis/electrochemical
conversion
• CO2 → Chem./Fuel
Coke and sinter production technology
• Improvement of
reduction efficiency
• Replacement of
C by H2
C reduction
Direct reduction 1 : Technology converting byproduct gas to reductant (CO2 Δ7%)
Direct reduction 2 : Biomass application
technology (CO2 Δ1%)
Indirect reduction:
Waste heat recovery/
CO2 utilization (CO2 Δ2%)
Exhaust heat recovery
• low/middle temp. exhaust
heat exchange
Sub 1 Project_Hybrid Ironmaking technology based on BF
Target: Develop Pilot Technologies to reduce CO2 Emissions by 10% in Ironmaking Process
Sinter
Sinter
plant

## Slide 3
Main Results
Sub 1 Project_Hybrid Ironmaking technology based on BF
 Sinter and Coke Manufacturing Technology
- Develop the sinter with high reduction degree using SiO2, size of limestone, and mixing method of coarse particle
- Develop the high strength coke using the increase of coal rank and bulk density of coal blend
 Pilot-scale Fluidized Bed Reactor (PFBR) for LRI Manufacturing : > 65%(RD)
- Design and construct the PFBR with dimension of 0.3m I.D., 3.3m height, 50 kg
- Operate the PFBR using multi-step method to simulate a multi-stage FBR
(R4, R3, R2, R1) with a single FBR
- Produce LRI with more than 78% of RD for Australian and Brazilian Ores
 COG Injection and LRI Charging Technology
- Develop a mathematical model for BF based on heat and mass balance
- Implement the tests in a BF shaft reaction tester(IReS) with reaction conditions calculated by model
- Avg reduction degree of burden material is higher using COG/LRI simultaneously
- In case of simultaneous COG injection/LRI charging, carbon consumption significantly decreases, and
CO2 reduction effect is 7.7% It is slightly higher than that of individual case of COG injection and LRI charging
[RAR]
[CO2 Reduction Effect]
[Overview of PFBR]
Synergy
Effect
CO2
Reduction
Target

## Slide 4
Future Project
○ Background
- Plan a national project to substantiate the key results of COOLSTAR project(P phase) in commercial BF
- Demonstrate the reduction of RAR in commercial BF(Ph No. 2) through H2 rich gas injection and alternative
iron charging
- BF : 2650 Nm3 (Pohang No. 2, POSCO)
- Targets
. Test of H2 rich gas injection : ≥ 65 Nm3/t-p
. Alternative iron charging : 5 %
- Analysis of BF operation and CO2 emissions reduction
‘30.12
’25.4
Construction for injection/charging facilities
Design of the operating parameters of BF
’27.12
○ Roadmap
Coke Oven
PCI
Coke
Sinter/Pellet
Pig Iron/Slag
COG
Compressor
Hot Stove
1200℃
NG Tank
DRI, HBI
LRI, Scrap
No. 2 BF Test
COOLSTARX (Apr. 2025 ~ Dec. 2030)