## Slide 1
〮 Flexible Feedstock Utilization
- Ferrous feeds can be fed without additional agglomeration
- Sintering, coke-making and pelletizing, etc.
〮 Enhancement of reaction efficiency
- Superior heat and mass transfer due to gas-solid contact
Melting
Fluidized Bed Reactor (FBR) Multi-stage reduction process
FINEX with fluxed sinter
≤8mm
Iron Ore
Direct use
Advantages of FBR
Challenges of FBR
〮 Melting behavior of DRI in electric melting furnace (EAF, ESF)
- Lack of flux → Poor assimilation behavior
〮 Slag Quality and Energy Demand
- Greater energy or flux demand may arise in EAF/ESF stages.
[Key concepts]
✔ Optimization of fluxing conditions and blending strategies is key to closing the loop for efficient FBR and melting furnace integration.